## Slide 1: Development of in-vitro test to determine corneal cell damage due to CL induced mechanical damage Greg Hofmann Philippe Jubin Pierre Gerligand Annabelle Gallois-Bernos Johnson and Johnson Vision Care, Jacksonville, FL, USA Steve Franklin Nicole Smulders Lutz-Christian Gerhardt Sanne Valster Philips Group Innovation, Eindhoven, NL
Measurements of the DCoF between human corneal epithelial (HCE) tissue (constructs) and contact lenses and the associated frictional forces were made using the system shown in Figure 1. The lenses employed in this test can be found in Table 1.
The exposed constructs were stained and imaged; the images were processed using a custom Matlab code to yield percent cell damage.
Frictional energy was determined by integrating (numerically) the frictional force over the corresponding sliding distance.
Mechanical interactions can result in damage to corneal epithelial tissue [1- 3]. Contact lens comfort is strongly associated with contact lens dynamic coefficient of friction (DCoF) data and frictional energy, or sliding work, may be related to comfort [4,5].
Several studies have examined these systems using micro-tribology; however, the contact pair used was either not relevant to lens-eye tribology or did not lend itself to cell damage assessment [6-12].
It is proposed that frictional energy (sliding work) is an appropriate metric for cell damage.
Introduction
©JJVCI, 2015. All rights reserved
Poster first presented at BCLA Conference 2015.
1 of 3
Methods
Construct
Mounting Pin
Holder Sleeve
Rubber Tip and Contact Lens Sample
Cantilever Flexure
Petri Dish
Maintenance Medium & TLF
Figure 1: Micro-tribometer and HCE construct used to obtain frictional force and DCoF data
Lens Material Contact Lens Brand | N | Mean Percentage Damage (SD) | Mean DCoF (SD)
balafilcon A PureVision® (PV) | 5 | 22.7 (6.1) | 0.064 (0.008)
etafilcon A with PVP 1-DAY ACUVUE® MOIST (1DM) | 3 | 12.6 (8.5) | 0.043 (0.006)
lotrafilcon A AIR OPTIX® AQUA (AOA) | 2 | 7.7 (1.9) | 0.057 (0.010)
comfilcon A Biofinity® (BF) | 3 | 13.3 (5.5) | 0.051 (0.001)
etafilcon A ACUVUE® 2 (Acv2) | 9 | 25.2 (11.6) | 0.068 (0.013)
narafilcon A 1-DAY ACUVUE® TruEye® (1DTE) | 3 | 6.8 (9.8) | 0.043 (0.001)
senofilcon A ACUVUE OASYS® (AO) | 10 | 13.6 (5.3) | 0.040 (0.007)
Table 1: HCE tissue cell damage and dynamic coefficients of friction for various contact lenses subjected to tribological rubbing.

## Slide 2: Development of in-vitro test to determine corneal cell damage due to CL induced mechanical damage Greg Hofmann Philippe Jubin Pierre Gerligand Annabelle Gallois-Bernos Johnson and Johnson Vision Care, Jacksonville, FL, USA Steve Franklin Nicole Smulders Lutz-Christian Gerhardt Sanne Valster Philips Group Innovation, Eindhoven, NL
An example wear track is shown in Figure 2.
Results
Cell damage and DCoF data were shown in Table 1.
Percent cell damage as a function of frictional energy is plotted in Figure 3.
600 microns
Figure 2: Wear track on epithelial tissue (between red lines). The contact lens material rubbed against the tissue was balafilcon A.
Figure 3: Plot of cell damage as a function of frictional energy delivered to HCE tissue surface. A correlation (Pearson’s R) of 0.62 (P<< 1%) was found.
©JJVCI, 2015. All rights reserved
Poster first presented at BCLA Conference 2015.
2 of 3

## Slide 3: Development of in-vitro test to determine corneal cell damage due to CL induced mechanical damage Greg Hofmann Philippe Jubin Pierre Gerligand Annabelle Gallois-Bernos Johnson and Johnson Vision Care, Jacksonville, FL, USA Steve Franklin Nicole Smulders Lutz-Christian Gerhardt Sanne Valster Philips Group Innovation, Eindhoven, NL
Lens brand was a significant factor for both cell damage (P ~ 1%) and DCoF (P << 1%).
A correlation between cell damage and frictional energy (0.62 P << 1%) was found.
DCoF comparisons to previous measurements were good and mixed [10-12]. Values for AO similar to those found by Dunn [10]. Comparisons to Tosatti [11] (Table 2) and Samson [12] mixed.
The frictional energy metric is likely more appropriate than DCoF for assessing corneal damage (mechanical) since frictional forces depend on many other factors: the ocular shape, eyelid pressures, and lens properties. Additionally, frictional energy metric accounts for mechanical cell fatigue and lens movement.
More work is needed to understand the relationship between the frictional energy metric and clinical outcomes.
Discussion and Conclusions
REFERENCES
Young, G and Mirejovsky D. A Hypothesis for Aetiology of Soft CL-Induced Superior Arcuate Keratopathy; ICLC, Vol. 20, September/October 1993.
O’Hare, N et al. CL – Ocular Surface Interactions in Superior Epithelial Arcuate Lesions (SEALS); Cornea Vol19(6) Supplement 2, November 2000 p2110 (Abstract)
Young, G, Coleman, S. Poorly Fitting Soft Lenses Affect Ocular Integrity; CLAO 2001
Brennan, N and Coles, C, CLAE, Volume 36, Pages e10, 1 December 2013.
Kakkassery, J et al. Evaluation of Frictional Forces and Dynamic Adhesion Properties of Commercial Silicone Hydrogel CLs; Poster: AAO, 2013.
Rennie, A et al. Friction Coefficient of Soft contact Lenses: Measurements and Modeling, Tribology Letters, vol. 18, 2005 pp. 499-504.
Zhou, B et al. A Study of Frictional Properties of Senofilicon-A Contact Lenses, J. Mech. Behavior Biomedical Mat. 4 (2011) pp. 1336-1342.
Dunn A et al. Lubricity of Surface Hydrogel Layers, Trib. Lett., Dec. 2012.
Roba M. et al. Friction Measurements on Contact Lenses in Their Operating Environment, Tribol. Lett. (2011) 44:pp.387-397.
Dunn A et al. Friction Coefficient Measurement of Hydrogel Materials on Living Epithelial Cells, Tribology
Tosatti S et al. Dynamic Coefficient of Friction Measurments of Contact Lenses in Tear Like Fluid, BCLA Abstract, 2014.
Samson M et al. Invitro Friction Testing of CLs and Human Ocular Tissues: Effect of Proteoglycan 4 (PRG4). Tribology International, 2014.
ACKNOWLEDGEMENT
This work was funded by Johnson & Johnson Vision Care, Inc.
1-DAY ACUVUE® MOIST, ACUVUE® 2, 1-DAY ACUVUE® TruEye® and ACUVUE OASYS® are registered trademarks of JJVCI. All others are trademarks of their respective owners.
CORRESPONDENCE
Johnson & Johnson Vision Care, Inc. (JJVCI) 7500 Centurion Parkway, Suite 100, W-2B,
Jacksonville, FL 32256, USA
Email: ghofmann@its.jnj.com
Lens Material Contact Lens Brand | Mean dynamic DCoF (std) 100 cycles | Tosatti et. al. [12] Mean DCoF (std) 100 cycles | Absolute Value of Difference
balafilcon A PV | 0.064 (0.008) | 0.231 (0.018) | 0.167
etafilcon A with PVP 1DM | 0.043 (0.006) | 0.024 (0.010) | 0.019
lotrafilcon A AOA | 0.057 (0.010) | 0.119 (0.105) | 0.062
comfilcon A BF | 0.051 (0.001) | 0.011 (0.005) | 0.040
etafilcon A Acv2 | 0.068 (0.013) | 0.041 (0.010) | 0.027
narafilcon A 1DTE | 0.043 (0.001) | 0.008 (0.009) | 0.035
senofilcon A AO | 0.040 (0.007) | 0.010 (0.015) | 0.030
Table 2: Summary of CoF Comparisons to Tosatti et. al. [11]
©JJVCI, 2015. All rights reserved
Poster first presented at BCLA Conference 2015.
3 of 3